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ClarkDietrich® Low-Embodied Carbon (LEC) Metal Lath and Accessories
Section 092400 – Cement Plastering
NOTE:
Turn on hidden text to view important non-printing notes by selecting Show/Hide (¶) in the Paragraph Group, or by using the Ctrl+* keyboard shortcut.
Note to Specifier: The language provided herein is intended to be supplementary to Division 09 Metal Lath Sections. It contains the necessary language for the specification of Low-Embodied Carbon (LEC) Metal Lath and Accessories only. Coordinate with Related Requirements in applicable Division 01 Sections.
PART 1 -  GENERAL
Retain Paragraph below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections. These may include “Section 013329 – Sustainable Design Reporting,” “Section 013563 – Sustainability Certification Project Requirements,” “Section 013566 – Sustainability Certification Project Procedures,” “Section 018113 – Sustainable Design Requirements” or related Sections.
1.1 SUMMARY
A. Related Requirements:
1. <Insert Section Number and Title>.
1.2 ACTION SUBMITTALS
A. Sustainable Design Submittals:
1. Low-Embodied Carbon (LEC) Environmental Product Declaration (EPD): For applicable products specified in Part 2.
a. Product-Specific Type III Environmental Product Declaration (EPD): Third-party verified, in conformance with ISO 14025 and EN 15804.
1) Global Warming Potential (GWP) values in kg CO₂e per declared unit.
PART 2 -  PRODUCTS
2.1 MATERIALS
A. Low-Embodied Carbon (LEC) Requirements:
1. Global Warming Potential (GWP) Thresholds: For [Metal lath] [Galvanized steel plaster accessories] complying with ASTM A653/A653M.
Maximum 2,228 kg CO₂e/ton cradle-to-gate is a recommended threshold determined by the U.S. General Services Administration.
a. Maximum 2,228 kg CO₂e/ton cradle-to-gate.
2.2 METAL LATH
A. [bookmark: _Hlk212726616]Expanded-Metal Lath: ASTM C847, cold-formed carbon-steel sheet with ASTM A653/A653M, G60 (Z180), hot-dip galvanized-zinc coating.
Retain "Basis-of-Design Product" Paragraph below to require a specific product or a comparable product from manufacturer listed.
1. Basis-of-Design Product: Subject to compliance with requirements, provide ClarkDietrich; Diamond Mesh Lath or comparable product by a current member of the SFIA.
2. [bookmark: _Hlk210025372]Diamond-Mesh Lath: [Flat] [Self-furring], [2.5 lb/sq. yd. (1.4 kg/sq. m)] [3.4 lb/sq. yd. (1.8 kg/sq. m)].
[bookmark: _Hlk203716074][bookmark: _Hlk176442631][bookmark: _Hlk203716055]3/8-inch (9.5-mm) rib lath is often used where its rigidity is necessary for long spans.
3. [bookmark: _Hlk203653732]High Rib Lath: 3/8-inch (9.5-mm) rib lath with herringbone mesh pattern; 3.4 lb/sq. yd. (1.8 kg/sq. m).
2.3 ACCESSORIES
A. General: Comply with ASTM C1861, and coordinate depth of trim and accessories with thicknesses and number of plaster coats required.
B. Metal Accessories:
Retain "Basis-of-Design Product" Paragraph below to require a specific product or a comparable product from manufacturer listed.
1. Basis-of-Design Product: Subject to compliance with requirements, provide weep and sill screeds, corners, casing beads, control joints and expansion joints by ClarkDietrich or comparable products by a current member of the SFIA.
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