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SECTION 092236 – LATH
or
SECTION 092400 – CEMENT PLASTERING
NOTE:
Turn on hidden text to view important non-printing notes by selecting Show/Hide (¶) in the Paragraph Group, or by using the Ctrl+* keyboard shortcut.
GENERAL
1.1 SUMMARY
A. Section Includes:
1. Metal lath.
2. Accessories.
1.2 ACTION SUBMITTALS
Retain "Sustainable Design Submittals" Paragraph below if required to attain sustainability rating or to track sustainability submittals.
A. Sustainable Design Submittals: For each product indicated.
"Construction and Demolition Waste Management" Subparagraph below applies to LEED v4 and LEED v4.1, MRc "Construction and Demolition Waste Management" and LEED v5, MRc5 “Construction and Demolition Waste Diversion.”
1. Construction and Demolition Waste Management: For each product.
PRODUCTS
1.3 MATERIALS
Retain "Recycled Content of Metal Lath" Paragraph below to specify recycled content if required.
"Recycled Content" Paragraph below applies to LEED v4, MRc "Building Product Disclosure and Optimization - Sourcing of Raw Materials,” LEED v4.1, MRc "Sourcing of Raw Materials" and LEED v5, MRc4 “Building Product Selection and Procurement.”
A. Recycled Content of Metal Lath: Postconsumer recycled content plus one-half of preconsumer recycled content not less than [25] <Insert number> percent.
1.4 METAL LATH
A. [bookmark: _Hlk204760777]Welded Wire Lath: ASTM C933, Class 1 galvanized coating complying with ASTM A641.
Per IAPMO UES ER-2017, Structalath III (1.0 lb/ sq. yd.) is a code-approved alternative to the 1.14 lb/ sq. yd. Welded Wire Lath specified in ASTM C933.
1. Product: Structa Wire, a ClarkDietrich Company; Structalath III or comparable product.
a. Weight 1.0 lb/sq. yd. (0.5 kg/sq. m).
Per IAPMO UES ER-2017, Structalath III 316 (1.0 lb/ sq. yd.) is a code-approved alternative to the 1.14 lb/ sq. yd. Welded Wire Lath specified in ASTM C933. Structalath III 316 features a 3/16-inch furring depth for one-coat stucco applications.
2. Product: Structa Wire, a ClarkDietrich Company; Structalath III 316 or comparable product.
a. Weight 1.0 lb/sq. yd. (0.5 kg/sq. m).
Per IAPMO UES ER-2017, Structa Twin Trac 2.5 (1.14 lb/ sq. yd.) is a code-approved alternative to the 2.5 lb/ sq. yd. Diamond Mesh Lath specified in ASTM C847 and the 1.14 lb/ sq. yd. Welded Wire Lath Specified in ASTM C933.
3. Product: Structa Wire, a ClarkDietrich Company; Structa Twin Trac 2.5 or comparable product.
a. Weight 1.14 lb/sq. yd. (0.62 kg/sq. m).
Per IAPMO UES ER-2017, Structa Mega Lath (1.95 lb/ sq. yd.) is a code-approved alternative to the 3.4 lb/ sq. yd. Diamond Mesh Lath specified in ASTM C847, the 1.4 lb/ sq. yd. Woven Wire Lath specified in ASTM C1032 and the 1.95 lb/ sq. yd. Welded Wire Lath Specified in ASTM C933.
4. [bookmark: _Hlk204760861]Product: Structa Wire, a ClarkDietrich Company; Structa Mega Lath or comparable product.
a. Weight 1.95 lb/sq. yd. (1.1 kg/sq. m).
Per IAPMO UES ER-2017, Structa V-Truss Walls and Ceilings (2.2 lb/ sq. yd.) is a code-approved alternative to the 3/8-inch, 3.4 lb/ sq. yd. High-Rib Lath specified in ASTM C847 and the 1.4 lb/ sq. yd. Woven Wire Lath specified in ASTM C1032.
5. Product: Structa Wire, a ClarkDietrich Company; Structa V-Truss Walls and Ceilings or comparable product.
a. Weight 2.2 lb/sq. yd. (1.2 kg/sq. m).
B. Stainless Steel Welded Wire Lath: ASTM C933, SS304 alloy wires complying with ASTM A555.
Per IAPMO UES ER-2017, Structa Stainless Steel Mega Lath (1.95 lb/ sq. yd.) is a code-approved alternative to the 3.4 lb/ sq. yd. Diamond Mesh Lath specified in ASTM C847, the 1.4 lb/ sq. yd. Woven Wire Lath specified in ASTM C1032, and the 1.95 lb/ sq. yd. Welded Wire Lath Specified in ASTM C933.
1. Product: Structa Wire, a ClarkDietrich Company; Structa Stainless Steel Mega Lath or comparable product.
a. Weight 1.95 lb/sq. yd. (1.1 kg/sq. m).
1.5 ACCESSORIES
A. General: Comply with ASTM C1861, and coordinate depth of trim and accessories with thicknesses and number of plaster coats required.
1. Exterior Corner Reinforcement - Profile: V-Truss [Straight] [Bullnose] [Arch] [One Coat] [Short Flange] Corner; fabricated from ASTM C933 welded wire lath with ASTM A641, Class 1 galvanized coating.
a. Product: Structa Wire, a ClarkDietrich Company; Structa V-Truss Corner or comparable product.
[bookmark: _Hlk506814792]Retain "Exterior Corner Reinforcement - Profile" Subparagraph below to require a V-Truss Straight Corner fabricated from stainless steel welded wire lath.
2. Exterior Corner Reinforcement - Profile: V-Truss Straight Corner; fabricated from ASTM C933 welded wire lath, with SS304 alloy wires complying with ASTM A555.
a. Product: Structa Wire, a ClarkDietrich Company; Structa Stainless Steel V-Truss Corner or comparable product.
1.6 MISCELLANEOUS MATERIALS
A. Fasteners for Attaching Metal Lath to Substrates: ASTM C1861.
Retain Subparagraph below for Stainless Steel Welded Wire Lath and Accessories.
1. Fasteners for Stainless Steel Lath and Accessories: Of same 300-series alloy as lath, or isolated from dissimilar metals with nonmetallic washers.
EXECUTION
1.7 INSTALLATION OF WELDED WIRE LATH
A. Installation: In accordance with ASTM C1063 and manufacturer’s evaluation report.
1.8 INSTALLATION OF ACCESSORIES
A. Install in accordance with ASTM C1063 and at locations indicated on Drawings.
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